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1. Dimensions/Volume/Weight
	Diameter
	241 mm

	Height
	595mm

	Volume
	20.5 L

	Weight (empty keg)
	2.61 kg


2. Materials
	Inner bag
	9 layers laminate, Multi layers high barrier

	Valve
	PA (food grade)

	Spear housing
	PA (food grade)

	Springs (food contact)
	Stainless Steel 304

	Springs (non food contact)
	Spring steel plated

	Seals
	TPE (food grade)

	Keg
	HDPE, glass fiber, epoxy

	Others
	PP


3. Shelf life and barrier performance
	Filled keg
	Depends on filled beverage and type of inner bag, up to 12 months

	O₂ pick up in 180 days
	< 0.8 ppm

	CO₂ loss in 180 days
	<10% (carbonization: 5.5g/L)

	Sealing of spear/inner bag
	≥6 bar, free of leakage

	Sealing of spear and keg
	≥6 bar, free of leakage

	Sealing of valve from outside
	≥2 bar, free of leakage

	Sealing of spear and metal coupler
	≥2 bar, free of leakage


4. Mechanical/physical Properties
	Operation temperature
	0°C ~ 45°C

	Maximum dispense pressure
	3.5 bar

	Strength at break
	≥15 bar, free of burst into pieces

	Piercing/stress strength
	≥10 bar, free of burst into pieces by piercing keg and/or with scratch mark

	Impact strength
	≥10 bar, free of burst into pieces by dropping from 2m height.

	Handle strength
	≥1 hour, no crack on handle of keg full filled.

	Strain strength
	≥10 bar, free of leakage of the keg body.

	Connection strength
	≥10 bar, no shooting out and/or damage of spear head.

	Opening pressure of safety valve
	8bar

	Closing pressure of safety valve
	6bar

	Maximum force loading on spear
	≥100 kg

	Disposal
	The Gprokeg is designed to give an extreme low impact on the environment, the empty keg is 100% recyclable, the product is 100% compliant to the EU Directive 94/62/EC


5. keg coupler type
	S Type (EU Sankey)
	D Type (US Sankey)
	A Type (German Slider)
	G Type (EU Sankey)


6. Food contact and microorganism
	Food contact approval
	All materials and additives used for the components intent to contact with food  comply with European regulation EU10/2011 and other regulations

	FDA
	All materials and additives used for the components intent to contact with food  comply with FDA cfr 175.300

	Flavor/taste stability
	All materials intent to contact with beverages are free of small molecular migration and free of chemical reaction with content of beverages, keeping flavor/taste stability of beverages.

	total numbers of colony for spear and inner bag
	0

	total numbers of Bacillus coli in spear and inner bag
	0


7. Filling and Dispensing
	Filling volume
	≥20.0 liters, beer temperature: 0°C ~ 3°C； filling pressure: 2.0bar

	beer dispensing
	No CO2 on top of inner bag comes out with beer together


8. Palletizing
[image: ]Empty keg
	Pallet size
	1200x1000x110mm, one-way

	No. of layers
	4

	Kegs per layer
	23

	Kegs per pallet
	92

	Orientation
	Upside up

	Packing size
	1230 (L) x 1100 (W) x 2470 (H)

	Weight
	265.2kg

	Pallets are wrapped with stretch film



Filled keg
	No. of layers
	4

	Kegs per layer
	23

	Kegs per pallet
	92

	Orientation
	Upside up

	Height
	2.47m

	Max. layers in warehouse
	8
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