3L mini

- Dimensions/Volume/Weight

| Diameter | 170 mm |
| --- | --- |
| Height | 251mm |
| Volume | 3.2 L |
| Weight (empty keg) | 0.65 kg |

- Materials

| Inner bag | 9 layers laminate, Multi layers high barrier |
| --- | --- |
| Valve | PA (food grade) |
| Spear housing | PA (food grade) |
| Springs (food contact) | Stainless Steel 304 |
| Springs (non food contact) | Stainless Steel 304 |
| Seals | TPE (food grade) |
| Keg | HDPE, glass fiber, epoxy |
| Others | PP |

- Shelf life and barrier performance

| Filled keg | Depends on filled beverage, up to 12 months |
| --- | --- |
| O₂ pick up per year | < 0.8 ppm |
| CO₂ loss per year | <10% (carbonization: 5.5g/L) |
| Sealing of spear/inner bag | ≥6 bar, free of leakage |
| Sealing of spear and keg | ≥6 bar, free of leakage |
| Sealing of valve from outside | ≥2 bar, free of leakage |
| Sealing of spear and metal coupler | ≥2 bar, free of leakage |

- Mechanical/physical Properties

| Operation temperature | 0°C ~ 45°C |
| --- | --- |
| Maximum dispense pressure | 2 bar |
| Strength at break | ≥8 bar, free of burst into pieces |
| Piercing/stress strength | ≥6 bar, free of burst into pieces by piercing keg and/or with scratch mark |
| Impact strength | ≥6 bar, free of burst into pieces by dropping from 2m height. |
| Handle strength | ≥1 hour, no crack on handle of keg full filled. |
| Strain strength | ≥8 bar, free of leakage of the keg body. |
| Connection strength | ≥6 bar, no shooting out and/or damage of spear head. |
| Maximum force loading on spear | ≥100 kg |
| Disposal | The Gprokeg is designed to give an extreme low impact on the environment, the empty keg is 100% recyclable, the product is 100% compliant to the EU Directive 94/62/EC |

- keg coupler type

| Specific coupler fit with Gprokeg specific dispensing/filling tool |  |
| --- | --- |

- Food contact and microorganism

| Food contact approval | All materials and additives used for the components intent to contact with food comply with European regulation EU10/2011 and other regulations |
| --- | --- |
| FDA | All materials and additives used for the components intent to contact with food comply with FDA cfr 175.300 |
| Flavor/taste stability | All materials intent to contact with beverages are free of small molecular migration and free of chemical reaction with content of beverages, keeping flavor/taste stability of beverages. |
| total numbers of colony for spear and inner bag | 0 |
| total numbers of Bacillus coli in spear and inner bag | 0 |

- Filling and Dispensing

| Filling volume | ≥3.0 liters, beer temperature: 0°C ~ 3°C； filling pressure: 2.0bar |
| --- | --- |
| beer dispensing | Foam height: 10mm~30mm, beer temperature: 3°C; dispensing pressure: 1bar |

- Palletizing

Empty keg

| Pallet size | 1200x1000x110mm, one-way |
| --- | --- |
| No. of layers | 10 |
| Kegs per layer | 46 |
| Kegs per pallet | 460 |
| Orientation | Upside up |
| Height | 2.53m |
| Weight | 291kg |
| Pallets are wrapped with stretch film |  |

Filled keg

| No. of layers | 10 |
| --- | --- |
| Kegs per layer | 46 |
| Kegs per pallet | 460 |
| Orientation | Upside up |
| Height | 2.53m |
| Max. layers in warehouse | 16 |