Spear bag （Pro & Eco）

- Dimensions/Volume/Weight

|  | 30L | 20L (pro) | 20L (Eco) | 18L (Pro) | 15L (Pro) |
| --- | --- | --- | --- | --- | --- |
| Diameter | 71.5 mm | 71.5mm | 71.5mm | 71.5mm | 71.5mm |
| Height | 530.0mm | 395.0mm | 560.0mm | 560.0mm | 475.0mm |
| Volume | 31.0 L | 21.0L | 20.5L | 19.0L | 16.0L |
| Weight | 0.24 kg | 0.21kg | 0.21kg | 0.21kg | 0.20kg |

- Materials

| Inner bag | 9 layers laminate, Multi layers high barrier |
| --- | --- |
| Valve | PA (food grade) |
| Spear housing | PA (food grade) |
| Springs (food contact) | Stainless Steel 304 |
| Springs (non food contact) | Spring steel plated |
| Seals | TPE (food grade) |
| Others | HDPE |

- Shelf life and barrier performance

| Filled keg | Depends on filled beverage, up to 12 months |
| --- | --- |
| O₂ pick up per year | < 0.8 ppm |
| CO₂ loss per year | <10% (carbonization: 5.5g/L) |
| Sealing of spear/inner bag | ≥6 bar, free of leakage |
| Sealing of spear and keg | ≥6 bar, free of leakage |
| Sealing of valve from outside | ≥2 bar, free of leakage |
| Sealing of spear and metal coupler | ≥2 bar, free of leakage |

- Mechanical/physical Properties

| Operation temperature | 0°C ~ 45°C |
| --- | --- |
| Maximum dispense pressure | 3.5 bar |
| Strain strength (inside keg) | ≥10 bar, free of leakage of the keg body. |
| Connection strength (inside keg) | ≥10 bar, no shooting out and/or damage of spear head. |
| Opening pressure of safety valve | 8bar |
| Closing pressure of safety valve | 6bar |
| Maximum force loading on spear | ≥150 kg |
| Disposal | The Ecorekeg is designed to give an extreme low impact on the environment, the empty spear/bag is 100% recyclable, the product is 100% compliant to the EU Directive 94/62/EC |

- Spear coupler type

| S Type (EU Sankey) | D Type (US Sankey) | A Type (German Slider) | G Type (EU Sankey) |
| --- | --- | --- | --- |

- Food contact and microorganism

| Food contact approval | All materials and additives used for the components intent to contact with food comply with European regulation EU10/2011 and other regulations |
| --- | --- |
| FDA | All materials and additives used for the components intent to contact with food comply with FDA cfr 175.300 |
| Flavor/taste stability | All materials intent to contact with beverages are free of small molecular migration and free of chemical reaction with content of beverages, keeping flavor/taste stability of beverages. |
| total numbers of colony for spear and inner bag | 0 |
| total numbers of Bacillus coli in spear and inner bag | 0 |
| DosAGe of irradiation | 10KGY |

- Filling and Dispensing

| Filling volume | ≥specified keg volume, beer temperature: 0°C ~ 3°C； filling pressure: 2.0bar |
| --- | --- |
| beer dispensing | No CO2 on top of inner bag comes out with beer together |

- Packaging

|  | 30L | 20L (Pro) | 20L (Eco) | 18L (Pro) | 15L (Pro) |
| --- | --- | --- | --- | --- | --- |
| Carton box size (mm) | 630x430x320 | 480x450x320 | 630x430x320 | 630x430x320 | 560x430x320 |
| Spear bag per box (pcs) | 50pcs | 50pcs | 50pcs | 50pcs | 50pcs |
| Gross Weight (kg) | 13kg | 11.5kg | 11.5kg | 11.5kg | 11.0kg |